What depth-resolved transient measurements on a SiC honeycomb solar receiver imply for reduced-order heat transfer closures

A. Melhim1 and K. E. Kakosimos2

1Texas A&M University at Qatar, Qatar

2Aristotle University of Thessaloniki, Greece; kkakosimos@auth.gr

# Abstract

Volumetric solar receivers are meant to absorb concentrated radiation in depth and pass it to a heat transfer fluid (herein air) with little loss from the irradiated face, yet tested absorbers have repeatedly fallen short of the models used to design them. Those models are usually validated against an outlet air temperature and one or two solid temperatures, and this work examines how much such data constrain the receiver's internal heat transfer. A silicon carbide honeycomb receiver with 100 square channels of 1.5 mm side was instrumented at several depths and tested in a high-flux solar simulator at three irradiance levels and channel Reynolds numbers of 23 to 94, and its fifteen heating and three cooling transients were reduced without fitting a thermal model to them.

The measurements locate the limitation on gas–solid heat exchange at the scale of the whole assembly. The apparent Nusselt number lies one to two orders of magnitude below the laminar duct value, and the transient response is governed by an effective capacitance of 275 ± 38 J K⁻¹, six to seven times that of the monolith alone. For modelling, the key result is that the number of transfer units rises with flow, as Renom+0.341,, whereas any single-stream model whose heat transfer coefficient is a fixed function of axial position requires it to fall as Renom-1.00. This sign disagreement cannot be removed by recalibration, and it points to the flow distribution across the receiver as the missing element. The same runs show that the usual validation data cannot detect this: depending only on which thermocouple represents the solid, the fitted correlation prefactor changes by a factor of nearly thirty and the identified capacitance spans 122 to 281 J K⁻¹. A model can therefore match the standard validation data while misrepresenting the receiver, which may explain part of the long-standing gap between predicted and measured absorber performance. Finally, we identify the measurements needed to convert these response indices into physical coefficients, primarily a properly ranged pressure drop across the monolith.

Keywords: volumetric solar receiver; silicon carbide honeycomb; local thermal non-equilibrium; number of transfer units; flow maldistribution; model validation

# Introduction

Volumetric solar receivers, one route to convert solar energy to thermal or chemical energy, distribute concentrated radiation into the depth of a porous or structured absorber so the solid temperature peak sits inside the material suppressing reradiation from the hot front surface and raising attainable outlet temperature. State of the art analyses anticipate thermal efficiencies above 75% with air outlet temperatures beyond 1000 °C, silicon carbide absorbers usable to 1500 °C where metallic meshes are confined to 800–1000 °C {Ávila-Marín, 2011 #6980}. Prototype performance over three decades has been uneven: the wire-mesh TSA absorber reached 85% efficiency at 700 °C outlet and the recrystallized SiC SOLAIR absorber 70–75% at 750 °C {Avila-Marin, 2019 #6981;Avila-Marin, 2018 #4948}, but Sulzer 1 delivered 68% against 80% predicted by its own design code, and Catrec 2 was destroyed attempting to raise its 460 °C outlet temperature {Ávila-Marín, 2011 #6980;Avila-Marin, 2018 #4948}. A recent review by {He, 2023 #7018@@author-year} states that the theoretical volumetric effect has not been validated by experiment, and that most tested absorbers perform worse than predicted, as {Avila-Marin, 2019 #6981@@author-year} had also reported.

The experimentalists' response has largely been to characterize and refine absorber designs: foams and fibre meshes {Fend, 2004 #6987;Fend, 2004 #6988}, graded-porosity wire meshes and SiC morphologies {Avila-Marin, 2018 #4948;Avila-Marin, 2022 #6979}, single- against multi-layer ceramic foams {Zaversky, 2018 #5198}, pore-diameter variations {Wang, 2021 #5188}, reticulated-porous-ceramic cavity receivers {Patil, 2021 #7009}, screen-printed and metallic-foil absorbers reaching 91.8% efficiency against 84.6–85.3% for the HiTRec SiSiC benchmark {Broeske, 2023 #7011}, and calorimetric benches across rectangular channel geometries {D’Souza, 2025 #7010}. These studies yield design recommendations on porosity, cell density, layering and channel aspect ratio from steady-state efficiency measurements (see the Supplementary Material, hereafter SM, section S1 for more details on experimental campaigns).

In parallel, the reduced-order modelling literature treats the receiver most commonly as a simple porous continuum or a single channel, despite the complexities, with coupled local thermal non-equilibrium and radiation models. {Kribus, 2014 #4947@@author-year} show an idealized absorber in local thermal equilibrium achieving above 95% efficiency at 800 kW m⁻² and 1000 °C, which is unrealistically optimistic against the roughly 70% achieved by real absorbers. {Fend, 2013 #5195@@author-year} reproduce an extruded SiC honeycomb to within 15 K in outlet temperature and two efficiency points, with the extinction coefficient of 2300 m⁻¹ measured independently by transmittance, but with the volumetric heat transfer coefficient computed from a finer single-channel model. {Avila-Marin, 2019 #5189@@author-year} develop homogeneous equivalent models with a P1 radiation approximation and close the gas–solid coupling with volumetric correlations of the form Nulv=aRebPrc, fitting the respective coefficients. Superposing separately computed conduction and radiation contributions fails to recover the coupled effective conductivity {Mendes, 2014 #6993}, and a Rosseland treatment can differ from discrete ordinates by up to 76% {Moro Filho, 2020 #6989}. Our own group {Salih, 2023 #6977} showed specular channel reflectivity flattens the source term and raises modelled efficiency to 96% against 85% for the commercial HiTRec-II geometry using a similarly simplified approach validated against a single data point. In all these approaches the gas–solid temperature difference is built into the formulation, and its magnitude is set by the volumetric coupling coefficient. That coefficient, however, is taken from a correlation for another geometry, computed from a finer-scale model, or fitted to a few measured points.

The channel-scale physics has been analysed more carefully outside the solar field, in the catalytic-monolith literature, and with its validity conditions stated explicitly. {Cornejo, 2020 #6985@@author-year} computed laminar convection in monolith channels under constant wall temperature and constant wall heat flux across Re of 50–600, showing that evaluating the Péclet number at the inlet, instead of using a local temperature, introduces errors of 50% or more, and that at high heating rates a minimum appears in the Nusselt–Graetz curve some 16% below the asymptotic value. Effective axial and radial conductivities are established for honeycomb substrates {Hayes, 2009 #6990}, and the multi-scale comprehensive studies note radiation is required to reproduce measured axial temperature profiles and that a thermocouple inside a monolith channel can be significantly affected by radiation even without blocking the channel {Hayes, 2021 #6991}. A 0.05 mm wall gap substantially reduces effective radial conductivity {Cui, 2018 #6999}, and a pseudo-continuous two-dimensional reduction reproduces full three-dimensional CFD to better than 0.5 K {Schlereth, 2014 #7000}. These results, however, rest on assumptions their authors state: flow equally distributed over all channels {Schlereth, 2014 #7000}, and the gas treated as static {Cui, 2018 #6999}. These assumptions can therefore be checked, and they do not hold for an absorber under a concentrated, spilling beam and potentially without a uniform flow across the channels.

None of the experimental or computational studies we reviewed measures an installed receiver through its transients and reads the governing quantities directly off the measurement, which matters because calibration data for a reduced-order model are almost always a gas outlet temperature with one or two embedded solid temperatures. {Capuano, 2016 #6984@@author-year} illustrate the consequence: reviewing four established DLR models against one reference experiment, they report predicted outlet air temperatures of 1050, 1048, 1057 and 1073 K against 972 K measured, and efficiencies of 0.78, 0.77, 0.79 and 0.81 against 0.69, attributing the gap partly to the difficulty of experimentally evaluating a mean air flow temperature. The four models agree with each other to within 25 K but differ from the experiment by 80–100 K, which indicates that this validation target does not discriminate between modelling choices.

First, this work provides a new experimental dataset (section 2) of eighteen transients (fifteen heating and three cooling), each recorded at nine axial and radial locations of a lab-scale receiver, for various gas flow rates and irradiance levels. Second, it presents an analysis framework (section 3) that reduces the measurements to dimensionless groups, identifies the receiver's constants from the transient eigenstructure, and tests the structure of reduced-order formulations against the measured exponent. Instead of fitting a coefficient's value by inverse calibration, the framework examines the direction in which the transfer-unit count moves as flow rises. Any formulation whose volumetric conductance is a fixed function of axial position requires that count to fall in proportion to 1/ṁ, whereas the measurement herein has it rising; because the disagreement is in sign, it is independent of the coefficient value. The framework also quantifies how much the identified coefficients depend on the researcher's choice of reference sensor, and therefore how far a conventional validation exercise constrains the model. The results (section 4) comprise a dimensionless characterization of the installed SiC honeycomb receiver; a measured wall-to-interior disequilibrium; identification of effective capacitance and loss conductance from transient eigenvalues with sensor-selection sensitivity quantified; and a similarity rescaling on which the fifteen heating transients collapse. Finally, the data and framework support two methodological findings (section 5): that validation against a gas outlet temperature plus one or two solid temperatures is largely uninformative for this class of receiver, and that a uniform-temperature or uniform-flux coefficient evaluated on the fixed channel geometry cannot reproduce its flow response at any calibration.

# Experiment

## Receiver and apparatus

The absorber is a monolithic silicon carbide honeycomb (Figure 1d) with a ten-by-ten array of square channels of 1.5 mm side and 0.40 mm web thickness, giving a 1.9 mm pitch, a 19.0 mm square frontal face of area 3.61 cm², an open frontal fraction of 0.6233 and an axial length of 137 mm. The measured mass is 40 g, which over the solid cross-section of 1.360×10⁻⁴ m² and the 137 mm length gives an effective bulk density of 2147 kg m⁻³, consistent with a recrystallized SiC of roughly one third internal porosity; this is the value used for every capacitance estimate below. The geometry is of the same family as the extruded SiC honeycombs and catalyst-carrier substrates characterized in the solar literature {Fend, 2004 #6987;Fend, 2013 #5195} and modelled in our earlier work {Salih, 2023 #6977}, with a channel size between the two quoted literature samples (1.43 and 2.18 mm) and a comparable web thickness.

The monolith is enclosed in an aluminum cavity (142 mm in diameter, depicted in Figure 1b, and utilized earlier as a plain solar cavity {Sarwar, 2015 #6994}) held in place with multiple layers of alumina felt insulation (by Shine Refractories), and irradiated through a wider circular aperture by a seven-lamp high-flux solar simulator (Figure 1a), each lamp being a 6 kW xenon short-arc unit; the apparatus and its optical characterization (Figure 1c) are described in detail elsewhere {Haseler, 2021 #7016;Abdellateif, 2023 #7017}. The receiver is operated in suction: cavity air is drawn in through the irradiated face, passes through the monolith to the exit plenum, and leaves through a rear flange cooled by a closed water loop held at 25 °C, so that the gas reaching the metering line is near ambient. The measured temperature drop across that flange is large, 15 to 442 K between the plenum probe and the station immediately downstream of it across the campaign, which is why no station in the return line is used as the inlet reference. Air is metered by four Aalborg GFC17 thermal mass-flow controllers (MFC) of nominal 0 to 5 sL min⁻¹ range, all carrying air, referenced to 21.1 °C and 1 atm, and the total flow is their sum. Four units were used in place of a single 0 to 20 sL min⁻¹ device because the manufacturer specification is ±1.0% of full scale over the whole 0 to 100% range with ±0.5% full-scale repeatability, so subdividing the range reduces the absolute error provided the unit errors are not fully correlated, and section 3.4 reports both correlation limits for that reason. Only one of the four MFCs carries a factory calibration for air; the other three are calibrated for different gases, so their indicated flow is converted, which scales each unit's air-equivalent range by its own conversion factor and takes the widest to 5.72 sL min⁻¹. Rather than rely on the manual's conversion factors, each unit was calibrated in place against a bubble flowmeter, which replaces the factors with a directly measured characteristic and leaves a residual proportional to reading. Both terms are carried in the uncertainty model of section 3.4. Per-unit readings span 0.69 to 5.72 sL min⁻¹, from the smallest set point the controllers hold (10% of nominal range, below which flow was not controllable) to full range, so neither term is negligible against the other. Because these are mass-flow devices reporting standard volumetric units, the mass flow follows from the reference density ρstd = 1.1996 kg m⁻³.

Figure 1 The experimental assembly: a) The seven-lamp high-flux solar simulator with the receiver mounted on its optical axis; b) Side view of the receiver, showing the cylindrical aluminium cavity and the thermocouple leads entering through its wall; c) Front of the receiver with the alumina-coated Lambertian target and the calibration sensors used for the flux mapping of section 4.6; d) View of the opened cavity (without most of the insulation layers), showing the silicon carbide honeycomb seated in alumina felt insulation. Sensor axial positions are given in Figure 2.

## Instrumentation

Figure 2 shows the piping and instrumentation diagram (P&ID), mainly the nine sheathed thermocouples (sensors/probes) characterizing the measuring campaign: six of type N (TCDirect UK) and three of type K (Omega UK). Of these, three probes (type N, OD 1.5 mm, length 150 mm) contact the monolith side wall at axial positions of 11, 58 and 107 mm, denoted T8, T12 and T11 (TI-8, TI-12 and TI-11 in Figure 2). Two probes (OD 0.5 mm, length 500 mm) sit in the interior, flow-exposed region at 58 and 107 mm, denoted T9 and T10. One probe, T3 (type N, OD 1.5 mm, length 300 mm), sits in the exit plenum and reports the outlet gas temperature. One further probe, T2 (type K, OD 1.5 mm, length 150 mm), sits in the surrounding insulation and is used in section 4.6 to assess thermal stationarity; the wall-to-insulation drop T12 − T2 is 310 to 770 K, so the insulation resistance dominates radial transfer. The remaining two probes, T15 and T16 (both type K) placed a few cm behind and beside the cavity, respectively, give the setup's mean ambient temperature, T_amb. They are the least drifting temperatures in the rig, warming by 1.6 and 1.8 K between the first two minutes of a run and its steady window against 3.3 K for the probe downstream of the gas cooler, so the inlet reference is taken from them. Substituting either probe alone for their mean moves every quantity identified below by less than a tenth of its Monte Carlo standard deviation. The distinction between the wall chain and the interior pair is central to this work. Sections 4.3 and 5.1 show that the two report materially different temperatures at the same depth, and that the choice of which is taken as the solid temperature changes every identified coefficient. Interior probe readings in similar geometries are known to be perturbed by the radiation field {Hayes, 2021 #6991}, which makes the choice of reference temperature important. Thermocouple tolerance is treated per IEC 60584 class 1, which sets the same limit for type N and type K (the greater of 1.5 K and 0.004|t|, with t in °C), and which at the hottest front-probe reading of 1204 K is ±3.7 K. Installation error for the three sheathed wall probes, comprising contact resistance against the monolith and radiative exchange with the cavity, is not quantified.

Differential pressure across the monolith is monitored with a Keller PD33X of ±200 mbar range and ±0.1% full-scale accuracy (PI-1 in Figure 2, hereafter DP1), hence an accuracy floor of ±0.2 mbar. Section 4.7 shows this to be of the same order as the entire expected monolith pressure drop, so the readings cannot resolve it. They are nevertheless reported because a corrective measurement has been devised (section 5.3), and the pressure drop can discriminate between the two mechanisms discussed in section 5.2.

Figure 2 Piping and instrumentation diagram (P&ID), with the letter codes and thermocouple type colour codes given in the panel.

## Campaign and reduction

Fifteen heating runs span three lamp configurations at nominal aperture irradiances of 456, 304 and 256 kW m⁻²: runs E67–E71 at 7.1 to 15.3 sL min⁻¹, E72–E76 at 4.5 to 18.3 sL min⁻¹, and E77–E81 at 4.5 to 13.8 sL min⁻¹ respectively. Three cooling transients, C69, C80 and C81 at 10.5, 6.6 and 4.5 sL min⁻¹, follow lamp shutdown of the heating runs E69, E80 and E81 respectively, with flow maintained. Two additional runs, E82 and E83, repeat E77 and E81; they are retained in the dataset for repeatability check but excluded from every fit reported here. All raw data are available in the work's repository (see Data Availability section).

Steady-state values are 120 s means at the end of each heating run. The length-averaged wall temperature is the length average of the piecewise-linear profile through the three wall thermocouples with constant extrapolation to the end faces,

Tw=0.2518 T8+0.3504 T12+0.3978 T11,

using the exact trapezoid coefficients for thermocouples at 11, 58 and 107 mm over 137 mm. Gas enthalpy differences are computed by trapezoidal integration of cpT between Tamb and the relevant gas temperature. The measured conditions of the fifteen steady runs are collected in Table 1.

Table 1 The 15 heating conditions (measured quantities and fixed averages) of the campaign ordered by irradiance then flow rate

| Run | G0 [kW m-2] | q [sL min-1] | Tamb [K] | Tw [K] | T3 [K] | T12-T8 [K] |
| --- | --- | --- | --- | --- | --- | --- |
| E81 | 256 | 4.53 | 297.8 | 700 | 550 | -9.4 |
| E80 | 256 | 6.61 | 296.6 | 686 | 561 | +25.8 |
| E79 | 256 | 8.04 | 296.7 | 669 | 560 | +39.6 |
| E78 | 256 | 10.01 | 298.1 | 643 | 554 | +54.0 |
| E77 | 256 | 13.85 | 297.1 | 589 | 525 | +58.1 |
| E76 | 304 | 4.53 | 296.4 | 908 | 647 | -97.9 |
| E75 | 304 | 6.95 | 296.7 | 911 | 681 | -29.1 |
| E74 | 304 | 9.03 | 296.5 | 896 | 697 | +13.8 |
| E73 | 304 | 13.17 | 296.9 | 840 | 694 | +56.6 |
| E72 | 304 | 18.32 | 296.4 | 757 | 653 | +60.7 |
| E71 | 456 | 7.13 | 300.8 | 1047 | 753 | -83.5 |
| E70 | 456 | 9.11 | 299.0 | 1045 | 779 | -31.1 |
| E69 | 456 | 10.50 | 296.7 | 999 | 770 | +11.5 |
| E68 | 456 | 12.50 | 298.7 | 979 | 773 | +35.1 |
| E67 | 456 | 15.28 | 296.3 | 935 | 764 | +53.5 |

# Analysis framework

This section defines the quantities to which the experimental data are reduced. All are computed directly from the measured records; no thermal or radiation model of the receiver is fitted to them. This approach yields steady state dimensionless groups treating the assembly as a single-stream heat exchanger (section 3.1), an effective capacitance and loss conductance identified from the transient decays (section 3.2), a rescaling that tests the lumped description those identifications presume (section 3.3), and the uncertainty accounting (section 3.4). Assumptions beyond the framework itself, and other reference choices, are stated where they enter. The section closes with the implementation details and the libraries and packages used (section 3.5).

## Dimensionless groups

Per-channel mass flow is ṁch=ṁ/100and the hydraulic diameter is the channel side, Dh = 1.5 mm. Gas properties are evaluated at T̄g=Tamb+T3/2 except the thermal conductivity in the Nusselt number, which uses the film temperature T̄w+T̄g/2, because, as noted in the Introduction, evaluating the Péclet number at the inlet instead shifts the apparent Nusselt–Graetz curve by 50% or more {Cornejo, 2020 #6985}.

The receiver is characterized as a single-stream heat exchanger following {Kays, 2018 #7020@@author-year}, with effectiveness (ε) and transfer-unit count (NTU)

ε=T3-TambTw-Tamb, NTU=-ln1-ε,

giving an apparent assembly-level coefficient happand Nusselt number:

happ=NTU mchcpPL Nu=happDhkTfilm.

Re is evaluated with ṁ/100, assuming equal division of metered flow among the hundred channels (an assumption that sections 5.2 and 5.3 argue is violated), so a nominal Reynolds number, Renom, is required. Similarly, NTUapp,happ and Nuapp are calculated algebraically from the outlet-plenum probe T3 and an axial wall average, in the absence of independently measured interfacial coefficients. All four are considered installed-receiver response indices, appropriate for the analysis herein but not transport coefficients transferable to another geometry; extracting physical coefficients is left to a companion modelling study.

Two qualifications apply. First, the ε–NTU relation is exact for a wall at fixed temperature, whereas here the wall spans up to 321 K between T8 at the front and T11 at the back, and the maximum sits in the interior: the axial profile inverts, with T12 above T8 in 10 of the 15 runs. The inversion's onset moves to higher flow as irradiance rises: the lowest flow at which it is observed is 6.6, 9.0 and 10.5 sL min⁻¹ at 256, 304 and 456 kW m⁻², bracketing interpolated onsets of 5.1, 8.4 and 10.1 sL min⁻¹ (Table 3). The bias is quantified in section 4.2. A side-wall inversion indicator ΔTw = T₁₂ − T₈ is used throughout: negative while the front-face probe is the hotter, positive once mid-depth overtakes it. Second, since happis defined through NTU, Nu(Re) is algebraically tied to ε(Re):

dlnNudlnRe=1+dlnNTUdlnRe+dlncp/kdlnRe.

Because cpis evaluated at the bulk mean and k at the film temperature the ratio cp/k is used in place of a Prandtl number. A fitted Nu(Re) exponent is therefore not independent corroboration of the measured ε(Re); the independent flow dependence is that of the transfer-unit count, which is examined in sections 4.2 and 5.2.

The apparent wall-to-interior disequilibrium is expressed by the Λ ratios below, at each of the two receiver depths (58 and 107 mm) used as a surrogate of gas–solid nonequilibrium in section 4.3:

Λ58=T12-T9T12-Tamb,  Λ107=T11-T10T11-Tamb.

Finally, four dimensionless groups are used in section 5.2 to characterize the transport regime: Biot number Bi=happtw/2kSiC, Graetz number GzL=DhRePr/L, axial Péclet group Re·Pr·L/Dh, and radiation–conduction number Nrc=4σT̄w³Dh/kT̄w.

## Transient identification

After lamp shutdown, during cooling runs, the assembly's temperature decays with a single slow mode. For each sensor (probe) the excess temperature over the second half of the record, and above 5 K, is regressed as lnT-Tambagainst time, and λ is the mean of the per-sensor slopes. Lumping the assembly's thermal behaviour into one capacitance Cefflosing heat to ambient through a conductance Klosswhile delivering enthalpy to the gas gives:

λ=εmcp+KlossCeff.

Regressing λ against the gas advective conductance x=εṁcp therefore identifies both constants from the slope and intercept without solving a more detailed model. Each cooling transient is paired with the heating run sharing its identifier (EXX/CXX) and takes that run's effectiveness.

Identifying a heat transfer property from a transient rather than from a steady balance is established practice for these materials: {Fend, 2004 #6987@@author-year} obtained volumetric heat transfer coefficients of porous absorbers from the delay and damping of a temperature wave passing through a sample. The same logic is applied here to the full assembly.

In principle the heating branch decays with the same eigenvalue, and lnTss-T is regressed against time in the same way. It differs in that the asymptote Tss is estimated from the tail of the same record, which forces a choice of fit window. We use the middle of that record, 0.07<u<0.45, where u=Tss-T/Tss-T0 is the fraction of the total rise still to come (1 at lamp-on, 0 at steady state). Earlier than u=0.45 the faster modes have not yet decayed; later than u=0.07 the remaining deficit is comparable to the uncertainty in Tss itself. The choice of window matters. Sweeping the window from (0.05, 0.35) to (0.20, 0.70) moves Ceff monotonically from 295 to 200 J K⁻¹ while r2 improves from 0.84 to 0.97, so fit quality cannot select it (see also SM S3). The probe set alone changes Ceff by more than a factor of two (discussed in section 4.4).

We therefore report cooling as the primary identification, since its asymptote is measured and it needs no probe rule once the source is removed; heating serves as a conditional consistency check, and a joint fit to all eighteen eigenvalues gives an overall estimate. Their disagreement is addressed in section 5.1.

## Similarity rescaling

If the lumped description holds, every temperature transient should collapse when time is rescaled on the identified eigenvalue as t*=t/τ with a time constant of τ=Ceff/εṁcp+Kloss. The factor ε enters τ because the effectiveness converts the metered flow into the conductance that appears in the eigenvalue; both the reference constants and the effectiveness are taken from the primary identification and from each run's own measured effectiveness. The resulting half-rise time is a property of the receiver's response shape; an ideal single-node system gives ln 2, so the departure from ln 2 measures how far the receiver is from single-state behaviour.

## Uncertainty

The uncertainty of the calculated quantities is propagated from each measurement, based on the instrument specifications, through each calculation step. Because the whole framework is implemented in scripts (see section 3.5), uncertainty is propagated by Monte Carlo simulation {Possolo, 2024 #7023} over many "realizations". One realization perturbs every measured input by a random draw from its specified error and repeats the entire reduction on the perturbed record; after testing various counts, four thousand realizations give a representative and count-independent ensemble for each derived quantity, whose spread is the reported uncertainty. Because each physical error is drawn once and applied wherever it acts, correlations between derived quantities are carried by the ensemble. Three kinds of uncertainty are propagated and reported separately: (i) instrument error, (ii) systematic bias, and (iii) estimator choice.

## Instrument (random and calibration) error

For the thermocouples, the IEC 60584 class 1 type N and K tolerance (the greater of 1.5 K and 0.004|t|) is a maximum permissible error, so it is read as a 95% coverage bound and is halved to a 1σ systematic term, drawn once per sensor per realization and shared across runs, with an independent 0.5 K drift term per run; viscosity and conductivity carry 2% and 1% perturbations.

The metered flow sums four controllers carrying roughly 25, 33, 28 and 14% of the total, and their error has two terms because the two available sources of information constrain different quantities: the manufacturer specification is ±1.0% of full scale with ±0.5% full-scale repeatability, an additive bound in absolute flow, while the in-house bubble-flowmeter calibration constrains the slope of each unit's characteristic and so contributes a term proportional to reading. Each unit's standard deviation is therefore σ=0.0025F²+0.025qu²1/2, drawn once per unit per realization and combined with each record's own measured shares. F is the unit's air-equivalent full scale, the nominal 5 sL min⁻¹ scaled by its gas-conversion factor; instead of using the four individual factors we assign every unit the widest, F = 5.72 sL min⁻¹, which over-states the additive term and is therefore conservative. The two terms (manufacturer specification and bubble-flowmeter calibration) have opposite flow dependence, so the relative uncertainty on the summed flow falls from 2.8% at the lowest campaign flow to 2.5% at the highest for fully correlated units, and from 1.4% to 1.3% for independent ones. The two limits agree to within 0.0001 on every exponent and 0.5 J K⁻¹ on every capacitance, so which of them is used is immaterial; hereafter the larger is quoted, treating the flow error as predominantly systematic.

All fitted-slope quantities are accompanied by the regression standard error. For the pooled correlation and the transfer-unit count of section 4.2 that standard error exceeds the instrumental term by an order of magnitude and is therefore used as the uncertainty; for the better determined grouped correlation it exceeds the instrumental term only 3.4-fold (SM S2 details the propagation).

## Systematic Bias

Systematic bias in the outlet gas thermocouple is propagated over a range much larger than the calibration error. T3, in the exit plenum, sits at a convective–radiative equilibrium between gas and hardware and reads neither bulk gas nor wall temperature; the bias is potentially of order tens of kelvin and is uncharacterized. Outlet temperature measurement has been identified as a principal source of the model–experiment gap in this field {Capuano, 2016 #6984}, and radiative bias has been demonstrated for thermocouples in monolith channels {Hayes, 2021 #6991}. T3 enters ε, NTU, happ, Nu, ε* and η directly. It reaches Ceff and Kloss only through the effectiveness, which forms the abscissa x=εm˙cp of the eigenvalue regression. Each of these therefore carries a δT3 = ±25 K band alongside its Monte Carlo interval, evaluated on the transient identification as well as on the steady groups. Section 4.4 evaluates it and finds the identified capacitance to be the quantity least sensitive to the outlet-thermocouple systematic. Its impact is further discussed in section 5.2.

## Estimator choice

Where more than one reduction path exists (estimator choice), as for the inversion threshold ε*, each is propagated separately. Specifically, section 4.1 reports ε* as estimated both by interpolation between bracketing runs and by global linear regression, and treats the difference as a systematic uncertainty.

## Implementation

The reduction and figure generation are implemented as two Julia 1.12.6 scripts (see Data Availability and Reproducibility), executed in the repository environment with dependencies fixed by `Project.toml` and `Manifest.toml`. `receiver_reduction.jl` reads the raw logger records and generates all reduced data, regressions, uncertainty estimates, tables and the JSON results archive using CSV 0.10.16 and DataFrames 1.8.2 for data handling, GLM 1.9.5 for linear regression, Roots 3.0.4 for scalar inversions, Optim 2.2.1 with ForwardDiff 1.4.1 for the multi-start conductance-profile fits, Interpolations 0.16.3 and Trapz 2.0.3 for property interpolation and enthalpy integration, and JSON3 1.14.3 for serialization. `make_figures.jl` imports the shared reduction definitions without rerunning the complete reduction, regenerates plotting traces from the raw records when required, and renders Figures 3–7 using PythonPlot 1.0.6 with Matplotlib 3.9.1. Dry-air properties at 1 atm are evaluated using CoolProp 8.0.0 through the Julia `CoolProp_jll` binary: the Helmholtz equation of state of {Lemmon, 2000 #7027@@author-year} supplies cp while the {Lemmon, 2004 #7026@@author-year} correlations supply viscosity and thermal conductivity, consistent with the formulations used by REFPROP. Because `PropsSI` is a scalar call whereas the two 4000-realization Monte Carlo cases evaluate these properties several million times, CoolProp is queried once when the script is loaded on a 1 K grid spanning 200–1600 K, after which the call sites use linear interpolation. The interpolation error remains below 10-6 relative over 250–1500 K, and the grid brackets the campaign range of approximately 294–1200 K, so no experimental evaluation requires extrapolation. The Monte Carlo propagation and multi-start optimizer use fixed random seeds; consequently, rerunning the scripts with the archived Julia environment reproduces the outputs, apart from possible last-digit differences between numerical-library builds.

# Results

The reduced quantities for every run, referred to throughout this section, are given in Table 2; the measured conditions they derive from are in Table 1.

Table 2 The per-run quantities that follow from the definitions of section 3 (reduction framework). Runs are ordered by irradiance then flow rate, as in Table 1.

| Run | Renom | GzL | ε | NTUapp | Nprof | Nuapp | Λ58 | Λ107 | ηnom |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| E81 | 25.1 | 0.192 | 0.628 | 0.988 | 1.065 | 0.0380 | 0.0472 | 0.0661 | 0.252 |
| E80 | 36.3 | 0.277 | 0.680 | 1.138 | 1.213 | 0.0642 | 0.0505 | 0.0751 | 0.385 |
| E79 | 44.2 | 0.338 | 0.707 | 1.227 | 1.296 | 0.0853 | 0.0528 | 0.0817 | 0.466 |
| E78 | 55.3 | 0.422 | 0.742 | 1.355 | 1.408 | 0.1197 | 0.0576 | 0.0907 | 0.565 |
| E77 | 78.5 | 0.600 | 0.781 | 1.518 | 1.540 | 0.1951 | 0.0635 | 0.1108 | 0.694 |
| E76 | 23.2 | 0.178 | 0.573 | 0.851 | 0.925 | 0.0282 | 0.0343 | 0.0547 | 0.297 |
| E75 | 34.7 | 0.266 | 0.625 | 0.982 | 1.058 | 0.0494 | 0.0374 | 0.0636 | 0.501 |
| E74 | 44.6 | 0.341 | 0.669 | 1.106 | 1.179 | 0.0727 | 0.0404 | 0.0714 | 0.681 |
| E73 | 65.2 | 0.499 | 0.731 | 1.314 | 1.369 | 0.1302 | 0.0455 | 0.0900 | 0.985 |
| E72 | 93.6 | 0.715 | 0.773 | 1.481 | 1.512 | 0.2162 | 0.0531 | 0.1144 | 1.223 |
| E71 | 33.8 | 0.259 | 0.607 | 0.933 | 1.011 | 0.0444 | 0.0306 | 0.0608 | 0.407 |
| E70 | 42.5 | 0.326 | 0.644 | 1.032 | 1.109 | 0.0627 | 0.0322 | 0.0664 | 0.554 |
| E69 | 49.4 | 0.378 | 0.674 | 1.120 | 1.192 | 0.0802 | 0.0340 | 0.0733 | 0.628 |
| E68 | 58.6 | 0.449 | 0.697 | 1.192 | 1.257 | 0.1027 | 0.0357 | 0.0812 | 0.750 |
| E67 | 72.2 | 0.553 | 0.731 | 1.315 | 1.369 | 0.1417 | 0.0374 | 0.0939 | 0.902 |

## Steady field, flow response, and the inversion criterion

The steady temperatures against flow at each configuration are shown in Figure 3, and the response is strongly graded in depth. Front-face wall temperature falls steeply with flow, at −33.2, −24.3 and −20.8 K per sL min⁻¹ at 456, 304 and 256 kW m⁻² with r² of at least 0.97; the mid-depth wall falls at half to two-thirds that rate; the rear wall barely falls, at −1.1, −1.9 and −5.2 K per sL min⁻¹ with r² of 0.07, 0.12 and 0.76. Outlet gas temperature is nearly flow-invariant at the two higher fluxes (+0.6 and −0.1 K per sL min⁻¹, r² ≤ 0.03) and falls only weakly at the lowest, at −3.1 K per sL min⁻¹. At 456 kW m⁻² the outlet gas spans 26 K across the flow range against 264 K for the front-face wall, a ratio of ten; at 304 and 256 kW m⁻² the spans are 51 K against 331 K and 36 K against 194 K respectively.

Figure 3 Steady and outlet gas temperatures against flow rate at the three lamp configurations.

Figure 4 presents the analysis of the axial temperature profile and, in particular, its inversion; Table 3 gives the condition at which the inversion occurs, expressed both as a flow rate and as an effectiveness ε. The side-wall profile inverts as flow increases, crossing zero within the tested range at all three configurations (Figure 4a), and the crossings collapse when expressed in effectiveness (Figure 4b). Two caveats apply before the threshold is read as a universal number. First, the inversion indicator is the difference between two side-wall probes, at 11 and 58 mm, so it locates a front-to-mid crossing along the receiver axis as measured on the wall. The true temperature maximum is three-dimensional and need not lie on that wall, since the light beam is Gaussian and carries radial gradients; the radial traverse proposed in section 5.3 would locate it. Second, the inversion threshold also depends on how the effectiveness is formed: ε* uses the length-averaged wall temperature, and section 5.1 shows that its value changes when the reference probe changes. ε* is therefore an operating criterion for this receiver and its instrumentation.

Table 3 Located inversion crossings at the three configurations, by local interpolation between the bracketing runs and by global linear regression, with the effectiveness at crossing.

| Nominal G0 [kW m⁻²] | q* local [sL min⁻¹] | ε* local | q* global [sL min⁻¹] | ε* global |
| --- | --- | --- | --- | --- |
| 456 | 10.12 | 0.666±0.002 | 11.08 | 0.673 |
| 304 | 8.36 | 0.655±0.002 | 10.32 | 0.673 |
| 256 | 5.08 | 0.642±0.003 | 3.69 | 0.628 |

The two estimators agree to within 0.02 in ε* (Table 3), but differ in where they place the crossing flow. At 256 kW m⁻² the global regression puts the crossing at 3.69 sL min⁻¹, 18% below the lowest flow run at that flux: only one of the five points in that group is below zero, and the indicator rises steeply from it before flattening, so a single straight line is too shallow at the bottom and carries the crossing outside the data. Local bracketing between the two runs that straddle zero keeps all three crossings inside the measured range and halves the ε* spread, from 0.045 to 0.024; it is therefore the estimator adopted here.

Figure 4 a) The side-wall inversion indicator ΔTw=T12-T8 against flow at the three configurations, with the located crossings; b) The same data against effectiveness, collapsing at ε*≈0.65; c) The wall-to-interior disequilibrium indices at 58 and 107 mm against Reynolds number, rising linearly within every flux group.

The data support a crossing at ε* ≈ 0.65, rising weakly from 0.642 to 0.666 as the flux rises 1.8-fold. The experimental parameter space is not sufficient to claim either flux independence or a resolved flux dependence. Although the 0.024 spread of effectiveness is well above the 0.002–0.003 Monte Carlo intervals (Table 3), it is still no larger than the difference between the two estimators. The form of the criterion is nevertheless robust, since the inversion depends on the fraction of the available wall-to-ambient temperature difference recovered by the gas and not on flow rate or flux separately. Its value, however, depends on the outlet probe: under the δT3 = ±25 K band, ε* at 256 kW m⁻² runs from 0.579 to 0.704.

## Assembly-scale heat exchange behaviour

According to {Shah, 1978 #7019@@author-year}, the fully developed laminar square-duct reference depends on the thermal boundary condition, with three standard cases for unity aspect ratio: NuT = 2.976 for a uniform wall temperature, NuH2 = 3.091 for a uniform wall heat flux both axially and peripherally, and NuH1 = 3.608 for a uniform axial flux with an isothermal perimeter, with the product f⋅Re=14.227 throughout. The two flux conditions differ only in whether the wall conducts heat around the channel perimeter. We adopt NuH2as primary reference, since interior channels see similar radiative and convective conditions on all four walls and thin webs make a peripherally uniform flux a better idealization than a uniform temperature, consistent with the negligible web Biot number reported below. Irrespective of the reference case, the measured Nuapp (see Table 2) is a factor of 14.3 to 110 below NuH2, comparably far below channel-level Nusselt numbers of order three to four computed for monolith channels under either boundary condition {Cornejo, 2020 #6985}. This points to heat exchange limited at the assembly scale, not necessarily at the channel (film) level.

Over the full campaign (Figure 5a), the apparent Nusselt number follows a power law,

Nuapp=3.14±0.11×10-4 Renom1.444,  r2=0.968, n=15,

with pooled (all data together) regression standard error ±0.072 and instrumental Monte Carlo term ±0.003; the regression term exceeds the instrumental one roughly twentyfold, so the residual dispersion is physical and not instrumental. Fitted separately per irradiance configuration the exponent is 1.440, 1.476 and 1.530 at 256, 304 and 456 kW m⁻² (r² ≥ 0.9996 each), so pooled scatter reflects a flux-ordered offset plus a weak monotonic trend in the exponent. A common-slope model with a separate prefactor per irradiance configuration gives exponent 1.472, regression SE ±0.011, instrumental term ±0.003, r² = 0.9993, and prefactors 3.24, 2.72 and 2.55 ×10⁻⁴ in the same order. This grouped model is reported as the primary correlation alongside the pooled fit, because it is the better determined of the two and because the data were acquired at three discrete irradiance levels.

Figure 5  a) Apparent Nusselt number against nominal channel Reynolds number, with the fully developed laminar square-duct literature reference NuH2=3.09and the band spanning the other two thermal boundary conditions, NuT=2.98 to NuH1=3.61 {Shah, 1978 #7019}. Solid lines are the primary common-slope grouping per irradiance level; the dashed line is the pooled (all together) single-fit; b) Profile-corrected transfer-unit count against Reynolds number (filled symbols) with the isothermal-wall identity -ln1-ε (open symbols), and the respective slope fit on Reynolds number (solid line), against the Re-1 requirement of a conductance that is a fixed function of axial position (dashed line).

As shown in section 3.1, the Nusselt exponent is the effectiveness trend plus a definitional unit, so the independent quantity is the transfer-unit count. Integrating the gas energy equation through the measured piecewise-linear wall profile with a uniform h, and solving for the N=hPL/ṁcp that reproduces each run's measured outlet temperature, gives (Figure 5b)

Nprof∝Renom+0.341,  ±0.004 (instrumental), ±0.040 (regression SE),  r2=0.846

These counts exceed the isothermal-wall identity values by 1.4% to 8.7%, largest at low flow where the axial wall gradient is steepest, and the identity itself gives NTUapp∝Renom+0.389±0.045. The wall temperature profile is not available over the full length, since the probes start at 11 mm and finish at 107 mm, leaving the front 11 mm and rear 30 mm of the monolith unmeasured. Of the six plausible extrapolations considered, four yield admissible profiles; the two using a full linear continuation of the rear gradient are excluded because, for five of the fifteen runs, they place the exit wall temperature below the measured outlet gas temperature, which no single-stream model can produce. All admissible extrapolations move the exponent at the ±0.01 level, two orders of magnitude below the disagreement discussed next (full analysis in SM S4).

The transfer-unit count increases with flow, which an entire class of models cannot reproduce. For a single gas stream exchanging heat with a solid whose volumetric conductance is any fixed function of axial position (i.e. h(z) independent of mass flow), the transfer-unit count is

N=1mcp0Lhz P dz ∝ m-1 ∝ Re-1

with no adjustable constant. Physically, a conductance fixed in position (a function of axial position only) has a fixed total over the monolith length, so raising the mass flow gives each unit of gas heat capacity a smaller share of it, and the exchanger must become less effective. Evaluated on the measured properties the requirement is −1.000 for a fixed Nusselt number and −1.016 for a conductance independent of temperature and flow, the two differing only through the temperature dependence of the gas properties; we write it as −1.00 below. The measured exponent is +0.341, a difference of 1.34 in the power of Re and of opposite sign. A mismatch in magnitude could be absorbed by recalibrating the coefficient, but no flow-independent h(z), of any magnitude or axial distribution, produces a transfer-unit count that rises with flow. The result is not an artefact of the outlet probe: under a uniform δT3 = ±25 K offset the exponent ranges from +0.320 to +0.377, remaining positive and more than eight standard errors from zero. This is one of the main results of this work and is discussed further in section 5.2.

The dimensionless groups defined in section 3.1 characterize the transport regime of the cases studied. Beyond Renom and GzL, which are given per run in Table 2, the remaining auxiliary groups are tabulated in SM S5. The web Biot number never exceeds 3.4×10⁻⁵, so the solid is isothermal across the web thickness, consistent with the high effective conductivities reported for honeycomb substrates {Hayes, 2009 #6990} and with SiC at the conductive end of the substrates compared by {Cui, 2018 #6999@@author-year}. The Graetz number reaches only 0.715; its reciprocal, x*=1/GzL, runs from 1.40 at the highest flow to 5.63 at the lowest, against a fully developed asymptote reached at x* of order 10⁻¹ {Shah, 1978 #7019}, so the thermal entry region occupies only a few percent of the channel length at every condition. The axial Péclet group is at least 1481, so axial gas conduction is negligible, and the radiation–conduction number is 1.53 to 5.57, so the solid redistributes absorbed energy axially by radiation, consistent with radiation being required to reproduce measured axial temperature profiles in monolith channels {Hayes, 2021 #6991}. Section 5.2 uses these groups to exclude candidate explanations of the flow response.

## Local nonequilibrium

Figure 4c presents the wall-to-interior disequilibrium at the two instrumented depths (58 and 107 mm), each normalized on its own wall-to-ambient difference. Both disequilibrium indices rise linearly with Reynolds number within every flux group and both are small in magnitude, Λ₅₈ spanning 0.031 to 0.064 and Λ₁₀₇ spanning 0.055 to 0.114. At 107 mm the three per-flux slopes agree to within ±2%, with values of 8.77, 8.55 and 8.38 ×10⁻⁴ per unit Re at 456, 304 and 256 kW m⁻² and r² of 0.997, 0.999 and 1.000. However, offsets are ordered by flux: Λ₁₀₇ = c(G₀) + (8.54 ± 0.36)×10⁻⁴ Re, a flux-invariant slope with a flux-dependent offset falling as flux rises, intercepts 0.0448, 0.0341 and 0.0301 at 256, 304 and 456 kW m⁻². A pooled single-intercept fit averages the offsets away, gives r² = 0.898 against the 0.997–1.000 achieved within groups, and inflates the slope's standard error ninefold. At 58 mm the same structure holds at roughly a third of the slope (1.81, 2.66 and 3.12 ×10⁻⁴ per unit Re; r² of 0.984, 0.999 and 0.992), with Λ₅₈ rising by 22%, 55% and 35% across the flow range at the three fluxes. The disequilibrium is thus a smooth, monotonic function of depth and flow, with no threshold within the tested range.

The T9 and T10 sheathed thermocouples are exposed to the gas flow, but they are not bulk-gas measurements. Each sits at a convective–radiative–conductive equilibrium among gas, surrounding solid and their own stems, and for this geometry a probe inside a monolith channel is known to be significantly perturbed by radiation even unblocked {Hayes, 2021 #6991}. Λ is thus an apparent wall-to-interior disequilibrium, not a true gas–solid nonequilibrium, and is best treated as a lower bound on the latter, since radiative loading biases the interior probe toward the solid and understates the true gas–solid gap.

Local thermal non-equilibrium is built into the two-equation porous-absorber formulations {Kribus, 2014 #4947;Fend, 2013 #5195;Avila-Marin, 2019 #5189;Moro Filho, 2020 #6989} and into heterogeneous monolith models {Hayes, 2009 #6990;Schlereth, 2014 #7000}, its magnitude following from an assumed or fitted volumetric coefficient. Here the gap grows with Reynolds number: the wall-to-interior probe difference widens as flow rises, while the integrated transfer-unit count (section 4.2) also rises. Read directly, both indicate a participating gas–solid contact that increases with flow; section 5.2 examines whether this reading holds.

## Transient identification and the energy budget

Figure 6 presents the transient analysis from which the receiver's thermal capacitance and loss conductance are identified, and Table 4 collects the resulting constants. The three cooling transients decay as a single exponential in all six receiver probes, with a per-sensor eigenvalue spread of 3.7% (Figure 6a). The abscissa x=εṁcp (the gas-side advective conductance) requires an effectiveness for each cooling run; referring each run to the heating state it decays from, with cp on that run's own tail temperatures, gives the primary identification (Figure 6b),

Ceff=275±38 J K-1,  Kloss=0.080±0.023 W K-1,  r2=0.986.

Figure 6 a) Cooling decays of all six receiver probes at three flows, normalized on the initial excess; b) The slow eigenvalue against gas advective conductance εmcp for the three identifications, the primary matched-effectiveness cooling points (filled symbols) and the pooled-effectiveness abscissa (open symbols); c) Similarity collapse of the fifteen heating transients on τ=Ceff/εmcp+Kloss, wall (in grey) and outlet gas (in red).

A pooled ε(q) correlation across all fifteen heating runs, averaging over the flux ordering of ε, gives 298 ± 42 J K⁻¹ and 0.095 ± 0.025 W K⁻¹ at r² = 0.964; the matched form is better-conditioned and 8% lower in capacitance. Both, however, rest on three eigenvalues and hence one degree of freedom. The joint fit to all eighteen eigenvalues gives 269 ± 30 J K⁻¹ and 0.098 ± 0.022 W K⁻¹ with sixteen degrees of freedom and r² = 0.899; heating-only identification on the deep and outlet probes gives 281 ± 35 J K⁻¹ and 0.114 ± 0.027 W K⁻¹. The spread, 269 to 298 J K⁻¹ (11%), indicates how well the dataset determines the capacitance (Figure 6b). The Monte Carlo mean of the matched capacitance, 280 J K⁻¹, sits above the point estimate because Ceff is the reciprocal of a slope fitted to three points; the point estimate is quoted, with the Monte Carlo standard deviation beside it.

Whichever estimate is taken, Ceff exceeds the bare monolith capacitance of 42.0 to 46.8 J K⁻¹ (from the measured 40 g mass and cp at 600–900 K) by a factor of six to seven. On this lumped description, roughly five sixths of the thermal mass governing the receiver's transient is attributable to the holder and insulation. The attribution is by subtraction: the absorber's own capacitance is measured and the rest is the remainder. The identification cannot resolve how that remainder divides between holder, insulation and the plenum hardware. The installed capacitance governs the transient behaviour of the assembly, and hence start-up and cycling estimates, but does not appear in steady-state characterization. This is one reason it is absent from a literature built on steady efficiency measurements {Fend, 2004 #6987;Fend, 2004 #6988;Avila-Marin, 2018 #4948;Avila-Marin, 2022 #6979;Zaversky, 2018 #5198;Wang, 2021 #5188}, and it cannot be recovered from absorber material properties alone. It also qualifies He, Du and Shen's claim that porous volumetric receivers have quick transient response and small thermal inertia owing to the short flow path of the heat transfer fluid {He, 2023 #7018}. This holds for the absorber alone (42–47 J K⁻¹), but not for the installed receiver, in which most of the responding thermal mass belongs to the surrounding hardware.

Transient behaviour has typically been characterized via a receiver time constant from outlet air temperature. The same review of He, Du, and Shen reports time constants of about 90 s (Sulzer), 70 s (HiTRec II), 365 s (Sandia foam), 660 s (CeramTec) and 600–840 s (SOLAIR), noting no standard exists {He, 2023 #7018}. A time constant, Ceff/x+Kloss, measured at one flow leaves numerator and denominator unseparated; the 70–840 s spread reflects that conflation. Here the two are separated by varying the advective conductance, which attributes the six- to sevenfold excess specifically to holder and insulation. Other studies have resolved the transient computationally. A coupled transient model has been applied to start-up, shut-down, clear-sky and cloud passage {Sharma, 2023 #7029}, and ray tracing with pore-scale simulation and PID control gives 7.0 s (air) versus 45.9 s (molten salt), rising 129% as mass flow falls threefold {Du, 2024 #6998}. Because a predicted time constant implies a predicted capacitance, the factor found here can only be captured if the holder and insulation are modelled explicitly.

Table 4 collects these constants with their Monte Carlo intervals. The loss conductance is bracketed between 0.080 and 0.114 W K⁻¹, with the heating tangent exceeding the matched cooling secant by 1.41×, consistent with a partly radiative loss path but only weak evidence for T³ dominance. Carried through the δT3 = ±25 K band, the primary determination moves over 271.3 to 280.1 J K⁻¹ and 0.0752 to 0.0843 W K⁻¹, and the heating determination over 262.0 to 299.2 J K⁻¹ and 0.1072 to 0.1200 W K⁻¹. The band widens the loss bracket to 0.075 to 0.120 W K⁻¹ while the capacitance spread remains dominated by estimator choice (the probe set used).

Table 4 Identified constants with Monte Carlo standard deviations, 95% percentile intervals and, for fitted slopes, the regression standard error alongside.

| Constant | Value | s.d. | 95% interval | Unit | Notes |
| --- | --- | --- | --- | --- | --- |
| Nuapp prefactor a (pooled) | 3.14×10-4 | 0.11×10-4 | [2.93, 3.37] | ×10-4 | 15 steady runs |
| Nuapp exponent, pooled | 1.444 | 0.003 | [1.438, 1.451] | – | instrumental MC; regression SE ± 0.072, r2=0.968 |
| Nuapp exponent, grouped (primary) | 1.472 | 0.003 | [1.466, 1.479] | – | instrumental MC; regression SE ± 0.011, r2=0.9993 |
| Nprof exponent (primary) | +0.341 | 0.003 | [0.335, 0.347] | – | instrumental MC; regression SE ± 0.040; fixed-Nu requirement -1.000 |
| NTUapp exponent (identity, superseded) | +0.389 | — | — | – | isothermal-wall identity; retained for comparison only |
| Inversion marker ε* @456 kW m-2 | 0.666 | 0.002 | [0.661, 0.670] | – | operational marker under the adopted wall convention; see §5.1 |
| @304 kW m-2 | 0.655 | 0.003 | [0.650, 0.661] | – | same |
| @256 kW m-2 | 0.642 | 0.003 | [0.635, 0.648] | – | same |
| Λ107 slope [Re-1] | 8.54×10-4 | 0.36×10-4 | [7.85, 9.27] | ×10-4 | common slope, per-flux intercepts |
| Ceff, cooling matched-ε (primary) | 275 | 38 | [219, 369] | J K-1 | n=3, r2=0.986 |
| cooling pooled-ε | 298 | 42 | [237, 402] | J K-1 | r2=0.964 |
| joint 18 eigenvalues | 269 | 30 | [221, 337] | J K-1 | r2=0.899 |
| heating deep probes | 281 | 35 | [226, 361] | J K-1 | 122 J K-1 if all six probes used |
| Kloss, cooling matched-ε (primary) | 0.080 | 0.023 | [0.045, 0.136] | W K-1 | secant conductance |
| heating deep probes | 0.114 | 0.027 | [0.071, 0.177] | W K-1 | tangent conductance |
| Monolith capacitance (measured mass) | 42.0 – 46.8 | — | — | J K-1 | 40 g × cp(600–900 K) |

## Similarity collapse

Rescaling time on τ=Ceff/εṁcp+Kloss, the lumped time constant, collapses all fifteen heating transients (Figure 6c). The length-averaged wall temperature reaches half its total rise at t* = 0.205, with a coefficient of variation of 16.9% across runs spanning a fourfold flow range and a 1.8-fold flux range. The outlet gas reaches half rise at t* = 0.635 with a coefficient of variation of 7.8%. A single slow mode therefore describes the late heating transient, and the offset between the two half-rise values quantifies the phase lag between solid and gas. This does not, however, establish a one-state response. The wall half-rise sits well below ln 2, the dimensionless half-rise value expected for a single exponential mode, while the outlet sits close to it. The wall therefore retains a faster component not represented by the lumped model, consistent with the faster modes excluded from the heating fit window in section 3.2. The collapse shows that the late heating behaviour of all runs is governed by a common flow-dependent time scale set by the slow eigenvalue. This time scale is the input that start-up, shutdown and control models require, although the receiver is not a one-parameter dynamic system.

## Delivered aperture irradiance

Most of the results are temperature-based and their interpretation does not depend on the absolute irradiance level; only the efficiency and the delivered power per unit mass do. The aperture irradiance is nevertheless an important quantity for solar receivers, so we examine whether the radiometric flux mapping and an apparent steady energy closure converge. The radiometric flux mapping is an established three-step characterization procedure, already applied to this simulator {Haseler, 2021 #7016;Abdellateif, 2023 #7017}, where an optical model of the lamp reproduces the measured flux map, and a coupled Monte Carlo heat-transfer model driven by that flux reproduces measured cavity temperatures to within 0.2% on average {Sarwar, 2015 #6994}. The measurements give the nominal values 456, 304 and 256 kW m⁻² that label the three configurations of Table 1. The apparent steady energy closure takes Kloss from section 4.4 and omits storage by assuming the assembly is stationary at run end. Both assumptions are weak: the insulation probe rises from 308 to 356 K across the campaign, with a decay far slower than any run window, and the energy closure also carries the T3 bias directly into the heat absorbed by the gas, Qgas. The closure formula, together with the gauge geometry, face-to-gauge ratios and correction details underlying both determinations, is given in SM S6. Evaluated at both ends of the Kloss bracket and averaged per configuration, the ratio of the energy-balance estimate of aperture power to its nominal radiometric value runs 0.988–1.133 at 456 kW m⁻², 1.148–1.323 at 304 kW m⁻² and 0.783–0.915 at 256 kW m⁻². The aperture irradiance is therefore not determined to a single value, and the quantities that depend on it, such as efficiency, are reported as spans based on 450–517, 304–402 and 200–256 kW m⁻² for the respective configurations.

Closing the residual requires a flow-dependent term in the energy budget, and peripheral flow bypass and channel-group maldistribution are two candidates consistent with the observations in section 4.2. Non-stationarity and a flow-dependent probe response are also plausible; all four are discussed in section 5.2.

## Pressure drop

The installed differential-pressure measurement is assessed against a flow-through monolith prediction, to establish whether it resolves the absorber's own pressure drop. The prediction follows the standard decomposition for an open-channel substrate (face contraction, core friction, hydrodynamic entrance, thermal acceleration and face expansion) {Shah, 1978 #7019;Kays, 2018 #7020}, with all metered flow through the 100 channels. Core friction uses the square-duct Poiseuille number of 56.91, integrated along the channel with temperature-dependent properties. The entrance contribution uses the incremental pressure-drop number and Shah's apparent friction factor {Shah, 1978 #7030}; together with the face and acceleration terms, which the monolith-reactor literature finds negligible for a slender single substrate {Cornejo, 2020 #7025;Cornejo, 2021 #7024}, it accounts for a small fraction of the total. The resulting prediction is 0.24 to 1.29 mbar, of which 95 to 99% is core friction. Steady-window means of the differential-pressure channel compare poorly with it: the measured signal exceeds prediction by 1.4 to 2.1 times at high flow (2.74 against 1.29 mbar at 15.3 sL min⁻¹), falls below it at the low-flow end of the 304 and 256 kW m⁻² configurations, and goes negative at the lowest flow (−0.02 against 0.24 mbar at 4.5 sL min⁻¹). A negative drop across a resistance in steady forward flow is physically impossible and indicates a zero offset on the transducer, whose ±0.2 mbar accuracy floor is the same order as the entire expected monolith drop of 0.24 to 1.29 mbar.

Pressure drop is the quantity by which the volumetric-receiver literature diagnoses honeycomb flow stability: absorbers whose loss is linear in velocity tend towards instability {Kribus, 1996 #7021}, whereas high-conductivity materials with a predominantly quadratic characteristic are stable {Becker, 2006 #7022}. Instability becomes possible when one pressure-drop level maps to more than one outlet temperature {Broeske, 2022 #7008}. Recent unheated monolith measurements place a honeycomb on the linear, instability-prone side of that axis: the first experimental validation of a dual-cell-density pressure-drop model finds a linear relationship between Reynolds number and pressure drop in every configuration tested, underestimating the drop as Re rises through entrance and exit effects {Reinao, 2025 #7004}, effects large enough at channel Re of 50 to 320 to require an explicit correction factor dependent on spacing and misalignment {Cornejo, 2024 #7003}. Our transducer spans the monolith plus plumbing and cannot separate the absorber's characteristic from these comparable losses. The measurements are retained because the shortcoming is removable and because section 5.3 identifies this quantity as the one that would discriminate between the two candidate mechanisms. SM S8 gives the per-run, term-by-term comparison in Figure S1.

# Consequences for reduced-order receiver modelling

## Information content of validation against limited gas and solid temperatures

The standard validation dataset for a volumetric receiver model is an outlet gas temperature with one or two embedded solid temperatures. Almost every campaign surveyed above reports two quantities, outlet air temperature and efficiency {Fend, 2004 #6987;Fend, 2004 #6988;Avila-Marin, 2018 #4948;Avila-Marin, 2022 #6979;Zaversky, 2018 #5198;Wang, 2021 #5188}, named by He and co-workers {He, 2023 #7018} as the two key indicators, who note that a non-uniform radiation distribution produces a non-uniform air temperature distribution requiring more thermocouples than campaigns typically deploy. Likewise, modelling studies calibrate and validate against the same quantities {Capuano, 2016 #6984;Fend, 2013 #5195;Fend,  #6995;Avila-Marin, 2019 #5189}, and recent practice has not moved past it {Broeske, 2023 #7011;Patil, 2021 #7009;Kumar, 2022 #7013}. Because the present campaign went beyond this standard instrumentation, it allows a test of how much the standard quantities constrain the conclusions. They constrain them only weakly.

First, the outlet gas temperature is nearly insensitive to the internal field: across the flow range T3 varies by 26–51 K while the front-face wall varies by 194–331 K (section 4.1). Its flow slope even changes sign between configurations. Interior and wall probes at the same depth differ by amounts that grow with flow, so no single solid temperature represents the section. In addition, the choice of solid reference probe changes every identified coefficient, as recomputing the same fifteen runs with only the reference thermocouple varied shows in Figure 7a.

Figure 7 a) The apparent Nusselt correlation recomputed against five different solid reference probes from the same fifteen runs (see Table 5): the prefactor spans a factor of 29.7 and the exponent 1.09 to 1.85; b) The effective capacitance from the same eighteen transients under four selected sets of probes, with the fit-window range and the bare monolith capacitance marked.

Table 5 The apparent Nusselt correlation and the inversion marker recomputed against five candidate solid reference temperatures from the same fifteen runs.

| Solid reference | ε range | Nu prefactor | Nu exponent | ε* (456/304/256) |
| --- | --- | --- | --- | --- |
| front wall only (T8) | 0.454 – 0.851 | 5.91×10⁻⁵ | 1.847 | 0.605 / 0.591 / 0.572 |
| mid wall only (T12) | 0.520 – 0.710 | 2.70×10⁻⁴ | 1.428 | 0.604 / 0.590 / 0.570 |
| wall quadrature (adopted) | 0.573 – 0.781 | 3.14×10⁻⁴ | 1.444 | 0.666 / 0.655 / 0.642 |
| wall + interior mean | 0.608 – 0.803 | 3.75×10⁻⁴ | 1.421 | 0.691 / 0.682 / 0.671 |
| interior probes (T9, T10) | 0.648 – 0.826 | 4.56×10⁻⁴ | 1.394 | 0.719 / 0.711 / 0.702 |
| rear wall only (T11) | 0.771 – 0.823 | 1.76×10⁻³ | 1.092 | 0.787 / 0.787 / 0.791 |

Table 5 shows that the prefactor spans a factor of 29.7, the exponent 1.09 to 1.85, and the inversion threshold 0.57 to 0.79, each row corresponding to a plausible probe selection and, in effect, to a different receiver. Interior and wall probes at the same depth differ by 21–55 K at 107 mm and 21–27 K at 58 mm. Probe effects of this kind are documented at channel scale {Cornejo, 2020 #6985;Hayes, 2021 #6991}, where they amount to tens of percent; at assembly scale the prefactor changes by a factor of 29.7. Transient identification is also under-determined: the same eighteen transients yield Ceff of 122, 269, 275 or 281 J K⁻¹ depending on probe subset and window, the window alone spanning 200–295 J K⁻¹ while r² improves (Figure 7b). The overall range is a factor of 2.3.

A model's agreement with such a dataset is therefore not evidence of correct internal physics, because the identified coefficient reflects sensor placement and will not transfer to a different geometry, scale or operating envelope. This may explain the literature observations that most tested volumetric absorbers underperformed predictions {Ávila-Marín, 2011 #6980;Avila-Marin, 2019 #6981}, that four models cluster within 25 K of each other and 80–100 K from experiment, with mean-air-temperature measurement named as a principal suspect {Capuano, 2016 #6984}, and that the equilibrium model is optimistic by over twenty efficiency points {Kribus, 2014 #4947}.

Other studies point in the same direction. {Iding, 2024 #7012@@author-year} reproduce the front temperature of the 1080-cup Jülich receiver to 6.78 K RMS and the behind-cup air temperature to 7.51 K, on a two-quantity dataset (single gas and solid temperatures). They report, however, that this per-cup performance does not carry to the array of receivers: the field resolves the irradiated surface to a few kelvin, but not the depth direction in which the identified coefficients are defined. Conversely, {Song, 2026 #7028@@author-year} resolve the interfacial coefficient in porous media at low Reynolds number by measuring solid and gas temperatures simultaneously at each of a series of axial stations and solving the discretized gas energy equation directly. They note that this inversion approach is ill-posed. They describe co-located gas and solid temperatures as a requirement for data integrity; the present results quantify the error incurred when the solid reference is chosen instead.

We therefore recommend that receiver-model validations use multiple gas and solid temperature transients at various depths and, where a subset must be used, state explicitly which solid temperature defines the reference. The sensitivity of the identified coefficients to that choice should be reported where the instrumentation permits, and the coefficients otherwise declared conditional on it. This is not an argument against reduced-order models, only a statement that the standard validation dataset cannot discriminate among them.

## Limits of uniform-temperature and uniform-flux heat transfer coefficients in reduced-order receiver models

In the reviewed studies, zero- and one-dimensional receiver models close the gas–solid coupling with a coefficient from a correlation derived for a duct with uniform wall temperature or uniform wall flux: a Churchill cross-flow correlation in the inlet region {Capuano, 2016 #6984}, volumetric forms Nulv=aRebPrc {Avila-Marin, 2019 #5189}, the Fu and Kuwahara forms {Moro Filho, 2020 #6989}, or Graetz-problem Nusselt and Sherwood numbers at constant wall temperature {Schlereth, 2014 #7000}. Every such model ultimately reduces to the single-stream form:

mcpdTgdz=hz P Tsz-Tgz,

Section 4.2 establishes the Re-1 requirement for a fixed conductance against the measured exponent of +0.341. Four local repairs were tested and each fails: a developing-flow correlation {Cornejo, 2020 #6985;Shah, 1978 #7019} scales h no faster than Re0.5 and worsens the disagreement; solid-side resistance is ruled out by Bi ≤ 3.4×10⁻⁵; axial gas conduction by Re·Pr·L/Dh ≥ 1481; and a uniform imposed flux is excluded because Nrc of 1.53 to 5.57 means the solid redistributes absorbed energy axially by radiation {Mendes, 2014 #6993;Moro Filho, 2020 #6989;Hayes, 2021 #6991}.

Reynolds exponents above unity are common for interfacial coefficients measured in porous media at these Re. {Song, 2026 #7028@@author-year} compile eight correlations for Re ≤ O(10²) with exponents from 0.2 to 1.97, including their own Nu=0.001Re1.66Pr1/3, and our 1.444 over Re = 23–94 falls within that range. Their coefficient is volumetric and particle-referenced and ours apparent and wall-referenced; the comparison shows only that superlinear exponents recur when such coefficients are measured at low Re, not that the values should agree. Our correlation is likewise not a channel correlation: it is an assembly-scale quantity in the same non-dimensional form, and its gap from the laminar channel value reflects how little of the structure participates.

The transfer-unit solution of section 4.2 assumes spatially uniform h, excluding only a constant-Nusselt closure and not every fixed h(z). To test the broader claim, h(z) is fitted across three families: a single conductance profile shared by all runs, a separate profile fitted per irradiance configuration, and a shared Nusselt profile using each run's own conductivity. None reproduces the fifteen measured outlet temperatures, and the failure is systematic: the residual correlates with ln Re at r = −0.95 to −0.997, falling 90 to 197 K per e-fold across the three families, i.e. ordered by flow. A fixed conductance over-predicts outlet temperature at low flow and under-predicts it at high flow in every family, a trend the ±25 K outlet-bias band cannot absorb; fit mechanics, node counts and per-run residuals are tabulated in SM S4. The test presumes the single-stream form, and so excludes only flow-independent conductance within it, and it inherits the bounded but unmeasured wall extrapolations; neither limitation affects the sign or flow ordering of the residual.

Read directly, the measurement indicates that the participating gas–solid contact grows with Reynolds number. Two confounders would, however, produce the same trend without any change in participation: an outlet-probe bias varying systematically with flow, and a departure from thermal stationarity varying with run duration and hence with flow. This campaign bounds neither, so the first two measurements recommended in section 5.3 are directed at them.

Physically, a single-stream model cannot represent the flow distribution in a multi-channel receiver. Two mechanisms can produce a transfer-unit count that rises with flow. Viscosity-driven redistribution at common pressure drop: hot core channels choke relative to cooler perimeter channels, so as flow rises the field cools, the viscosity contrast weakens, and the participating fraction grows, predicting transfer units and the wall-to-interior deficit both rising with Re, as observed in sections 4.1–4.3, matching the viscosity-driven coupling reported for porous SiC absorbers {Wang, 2021 #5188}. Peripheral bypass: a leakage path through the housing clearance whose share falls as flow rises, being cooler with weaker temperature dependence, gives the same sign while inflating a nominal Reynolds number. The two cannot be distinguished from temperature data alone: redistribution keeps all flow within the channels, whereas bypass diverts part of it around them.

The first mechanism is related to the flow-instability criterion of the volumetric-receiver literature (section 4.7; {Broeske, 2022 #7008;Kribus, 1996 #7021;Becker, 2006 #7022}), which Ávila-Marín's review extends to highly porous honeycombs {Ávila-Marín, 2011 #6980}. Here the same mechanism acts in a stable regime: the viscosity-dominated contrast that drives runaway overheating in an unstable absorber would, in a stable one, redistribute flow reversibly as flow rises. The parallel-channel literature offers similar observations, qualitative only because both results concern flow boiling: lateral channel-to-channel conductance alleviates maldistribution {Rahman, 2024 #7015}, consistent with radial heat transfer reducing instability probability in porous absorbers {Becker, 2006 #7022}, although a maldistributed state can be thermodynamically favoured over an even one {Aka, 2024 #7014}. The radiation–conduction number measured here represents such a lateral conductance, so the rising transfer-unit count is observed together with a stabilising mechanism.

A more promising remedy than an improved Nusselt correlation is a multi-stream or distributed formulation with a pressure-coupled flow split, as used in pseudochannel models for flow maldistribution {Chanda Nagarajan, 2025 #7007}, flow-distribution models for dual-cell-density monoliths {Reinao, 2023 #7002} and dual-zone packed beds {Díaz, 2025 #7001}, and solar-field models at panel and module scale {Kumar, 2022 #7013;Schwager, 2024 #7005}. A flow-dependent split needs an inertial contribution or a path-to-path viscosity difference: a Darcy-only monolith split depends only on geometry, not flow {Reinao, 2023 #7002}, while an Ergun inertial term makes it Reynolds-dependent {Díaz, 2025 #7001}; the heated absorber carries a non-uniform viscosity field {Wang, 2021 #5188}, the viscous-to-inertial transition anchors the stability criterion {Kribus, 1996 #7021;Becker, 2006 #7022}, and buoyancy is a third such agent in molten-salt panels {Schwager, 2024 #7005} (SM S7). The data therefore rule out a single-stream formulation whose volumetric conductance is a fixed function of axial position, but not continuum models in general: such models reproduce three-dimensional CFD to better than 0.5 K under uniformly distributed flow {Schlereth, 2014 #7000} and obtain effective radial conductivities with a static gas {Cui, 2018 #6999}, which is reasonable for metered, uniform inflow. What fails here is their application under a concentrated, spilling beam, where the boundary conditions do not control the flow split.

## Measurements to resolve the open questions

Three measurements, ranked by value per unit cost, would resolve the remaining questions. Most valuable is a differential pressure measurement across the monolith faces alone with a ±2 to ±5 mbar transducer. The two candidate mechanisms of section 5.2 produce different pressure-drop characteristics at the same total flow. A pressure-drop series across the flow range would discriminate them, preferably run with a sealed-clearance control to remove the bypass path. A single point would not, since the two mechanisms differ in the flow dependence of the characteristic. The expected signal is 0.20 to 1.0 mbar, resolvable to a few percent with an appropriately ranged transducer. It would also connect this receiver to the permeability and Forchheimer characterization that the homogeneous-equivalent modelling literature depends on {Avila-Marin, 2019 #5189}. Further, it would place the absorber on one side or the other of the linear-versus-quadratic flow-stability criterion {Broeske, 2022 #7008;Kribus, 1996 #7021;Becker, 2006 #7022}. Such a measurement is practicable at this scale, as shown by a calorimetric test bench for pressurised gas receivers carrying absolute pressure sensors before and after the absorber alongside the thermocouples {D’Souza, 2025 #7010}. No measurement of channel-to-channel flow split in an irradiated honeycomb absorber appears in the recent literature. {Broeske, 2023 #7011@@author-year} state that individual mass-flow measurements for each of their sixteen absorber modules were impossible for reasons of space, so efficiencies were evaluated through radiative energy balance. The nearest published measurements isolate the effect in surrogates, varying air velocities in a two-tube fluidised-particle receiver at ambient temperature to impose controlled thermal heterogeneity and observe the resulting particle mass-flow split {Sahuquet, 2024 #7006}.

Second is an independent determination of outlet enthalpy, by mixing calorimeter or shielded aspirated probe. This would remove the T3 dependence that propagates into effectiveness, transfer units, the Nusselt correlation, the inversion threshold, efficiency, and the identified constants. It would address the mean-air-temperature difficulty named as a principal source of the field's model–experiment gap {Capuano, 2016 #6984}.

Third is a radial thermocouple traverse at one depth to resolve the core-to-perimeter solid profile, since section 5.1 identifies a single solid temperature per depth as the main limitation on identifiability. Two radial positions at one depth would test the redistribution mechanism directly and replace the reference-choice sensitivity of Figure 7a with a measured profile.

## Limitations

The main limitations, most of them stated where they arise, are: the isothermal-wall ε–NTU approximation and its profile correction (sections 3.1 and 4.2), and the unmeasured wall extrapolations (SM S4), of which the rear is bounded by the outlet temperature but not determined by it. The wall probes' installation error is unquantified. The outlet-probe bias is bounded only for a uniform offset; a flow-varying bias is unbounded and would act on the exponents. Thermal stationarity at each heating window's end is assumed but could not be demonstrated, and the primary transient identification rests on one degree of freedom. The inversion threshold at 256 kW m⁻² is as sensitive to the crossing estimator as to flux, and that group contains a single negative point. Despite the established flux-mapping procedure, the flux-map uncertainty is characterized only by its discrepancy with the energy closure. Two thermal models are solved, the profile-corrected transfer-unit count and the fixed-conductance falsification of section 5.2, and both integrate a single-stream gas energy equation through the measured wall profile.

# Conclusions

This work set out to characterize a structured silicon carbide volumetric receiver through its transient as well as its steady response, and to establish how far the measurements commonly used to validate receiver models constrain them. A honeycomb monolith instrumented on its side wall, within the monolith and in the outlet plenum was tested in a high-flux solar simulator at three irradiance levels, and its fifteen heating and three cooling transients were reduced without fitting a thermal model to them.

First, heat exchange between gas and solid is limited at the scale of the assembly rather than in the channel. The apparent Nusselt number scales as Renom1.472±0.011 but stays well below the laminar value NuH2 = 3.091, and a web Biot number of at most 3.4×10⁻⁵ excludes conduction through the webs, though not every solid-side or assembly-scale resistance, as the limiting step. The side-wall profile inverts once the gas has recovered about two thirds of the available temperature difference, at ε* of 0.642 to 0.666, and the wall-to-interior disequilibrium grows linearly with flow.

Second, the receiver transient is governed mainly by thermal mass outside the absorber. The slow eigenvalue identifies an effective capacitance of 275 ± 38 J K⁻¹, six to seven times the 42–47 J K⁻¹ of the bare monolith, and on the resulting time constant all fifteen heating transients collapse to a wall half-rise at t* = 0.205 within 16.9%, a single flow-dependent time scale for start-up and control models.

Third, the transfer-unit count increases with flow, as Renom+0.341±0.040, where a single-stream formulation with a volumetric conductance fixed in axial position requires Renom-1.00. The sign disagreement rules out that model class for this receiver, though not continuum models in general. Provided neither the outlet-probe bias nor thermal stationarity varies with flow, which this campaign could not verify, the missing element is likely the distribution of flow among the channels.

Fourth, the data commonly used for validation cannot detect such a failure. The choice of thermocouple representing the solid alone moves the identified Nusselt prefactor by a factor of 29.7 and the inversion threshold from 0.57 to 0.79, while probe subset and fit window move the capacitance from 122 to 281 J K⁻¹. A model can therefore fit an outlet temperature and one or two solid temperatures and still be structurally wrong, which may explain part of the long-standing shortfall of measured absorber performance. Validations should therefore use gas and solid transients at several depths.

Finally, the delivered aperture irradiance could not be fixed to a single value, so efficiency is reported as a span over 450–517, 304–402 and 200–256 kW m⁻²; the temperature-based conclusions do not depend on it. The measurement that would most advance this work is a pressure drop across the monolith faces alone: the installed transducer's ±0.2 mbar floor cannot resolve an expected 0.24 to 1.29 mbar, whereas a ±2 to ±5 mbar transducer would separate viscosity-driven redistribution from peripheral bypass.

# Data availability and reproducibility

The raw data for the experimental campaign described herein, as well as the programmed algorithms and scripts (see section 3.5 for more details) are available at the public repository https://github.com/auth-transp/transp-receiver.

# Acknowledgements

This work, and in particular Ms Aysha Melhim, was supported financially as an ExxonMobil Low-Carbon Research Fellow during her MSc studies at Texas A&M University at Qatar. The authors also wish to extend their gratitude to Dr. Jayanth Balasubramanian, Carbon Management Program Lead at ExxonMobil Qatar Limited, for his continuous support and insightful contributions during the fellowship. Finally, earlier parts of this work were supported by an NPRP award (NPRP12S-0301-190191) from the Qatar National Research Fund (a member of the Qatar Foundation).

# Declaration of Generative AI and AI-assisted technologies in the writing process.

Authors disclose the use of multiple AI tools during the preparation of this manuscript. LeapSpace (actual version is not publicly available) by Elsevier was utilized to identify and collect literature beyond the traditional search engines (e.g. Elsevier Scopus and Google Scholar). Claude Opus 5.5 by Anthropic through the Claude Science platform was utilized to cross-examine all the claims herein against the collected and referenced literature, and improve syntax and grammar of the text. GPT Sol (v5.6) by OpenAI through the Codex platform was utilized to improve and clean up the source code of the programming scripts, and the same scripts were reviewed by Gemini (v3.8) by Google through the Antigravity platform. The latter was employed to prepare a clean documentation to accompany the code at the public repository. The authors reviewed and revised the material generated (text and code) and take full responsibility for the content of this publication.

# References